SEMPU 1200 TX 1K

POLYURETHANE LOW VISCOSITY LIQUID MEMBRANE

www.sempoly.com

USES

3

DESCRIPTION

1

SEMPU 1200 TX  1K is single component, thixotropic liquid membrane which cures with the humidity in the air and developed for easpacially vertical uses.

ADVANTAGES

2

- Vertical application of roofs, terraces and gutters.

- Asphalt membranes.

- On light roofs made of metal and fibrous materials.

- Undertile applications in wet areas (kitchens, bathrooms e.t.c

- Thixotropic and easy to apply,

- Non sagging on vertical surfaces.

- Excellent mechanical properties; high elongation ability, tensile,

tear and abrasion resistance.

- High crack bridging properties.

- Preserves its mechanical properties between -40°C and +90°C.

- It is permeable to water vapor. Having a breathable structure is

does not cause accumulation in the substrate.

CONSUMPTION

4

Minimum total consumption: 1,5kg/m2

PACKAGING

5

5 and  25 Kg in metal buckets.

TECHNICAL SPECIFICATIONS

7

| QUALIFICATIONS | FEATURES | METHODS |
| --- | --- | --- |
| Color | Grey | - |
| Density | 1, 35±0,05 g/cm3 | ASTM D1475 / DIN 53217 / ISO 2811, 20oC |
| Shore | 50-60 Shore A | ASTM D2240 / DIN 53505 / ISO R868 |
| Viscosity | 15000-20000 cP | ASTM D 2196-86 / EN ISO 3219 (+25°C) |
| Adhesion to Concrete | 2,0- (N/mm2) | ASTM D4541 |
| Tensile Strength | 4,0- (N/mm2) | ASTM D 412 |
| Elongation At Break | %500 | ASTM D412 / EN-ISO-527-3 |
| Water Vapor Transmission | 0,8 gr/m2 hr | ASTM E 96 |
| Tack Free Time | 6-12 hours | - |
| Recoat Time | 6-24 hours | - |

* Viscosity measured at + 25°C according to EN ISO 3219 standards. Viscosity increases inversely with temperature.

APPLICATION PROCEDURE

7

Surface Preparation & Concrete Standards

Strength: C20/25.

Humidity: W ≤ 5%.

Temperature: 5-35 oC.

Relative humidity: < 85

The substrate must be clean, dry and free of all contamination such as dirt, oil, grease, and coatings etc. All dust, loose

and friable material must be completely removed from all surfaces before application of the product, preferably by brush

and/or vacuum.

Priming

- For porous substrates:  SEMPU PRIMER 1K, SEMPOXY PRIMER WB and SEMPU PRIMER 2K

- Metal or non porous surfaces: SEMPOXY PRIMER 1100

Application

The mixture should be applied by brush, roller or airless spray covering all surcafe properly.

SHELF LIFE AND STORAGE

8

Can be kept for minimum 12 months in the original unopened pails in dry places and at temperatures of 5-25 oC. Once a pail has been opened, use as soon as possible.

PRECUATIONS

9

Flammable and explosion products should be kept away during the application. Protective gloves and masks should be used for hands and eyes during application. The product should be used in well ventilated environments. If the material comes into contact with eyes, it should be washed immediately with sucient water. Children should kept away from the product. For more detailed information, ask for the Safety Data Sheet (MSDS).

.

The technical data and application methods given above are presented as a result of tests and applications carried out within the company. Considering that the conditions depending on the ground, weather conditions and humidity may vary during the application of the products, detailed examination and purposeful applications should be decided after examination by authorized persons in order to understand whether they will meet the special requirements and purposes before each application. The correct application of our products is your sole responsibility and liability. We will provide products with continuity and consistent quality under our general terms of sale and delivery. Users are responsible for compliance with local laws, the environment and obtaining permits from the necessary authorities. The new edition of the technical data sheet supersedes the previous edition. Ask your authorized sales representative for the current edition.